Photo-BCB process using 4024-40 BCB

- Deposit 180nm PECVD SiN for good adhesion of BCB.

- Take out small BCB bottle from freezer and warm up overnight

- Place sample in PEII at 100W, 300mT for 20s

- Dip HCl:DI 1:10 for 60s, Rinse in DI 60s, Blow Dry

- Apply AP3000 BCB Adhesion promoter, wait 30sec, and then spin 3krpm for 30sec

- Spin BCB ( step1:500rpm-400rpm/s-10sec ; step2:4000rpm-1000rpm/s-30sec)

- Soft Bake@80C/90sec

- Expose 2.2” in Autostep200 with focus 0

- PEB @55C/30sec\

- Immediately do puddle development using POLOS spinner program "7" ( step1: 500rpm-10sec; step2:4000rpm-400rpm/s-60sec)

  - Apply DS2100 BCB developer on quarter, wait 60sec, then run program “7”

  - While it is spinning @500rpm/10sec gently apply DS2100 (drop by drop in the center of the quarter)-Rinsing step (first part of recipe 7 described above)

  - Spin dry at 4000rpm/60sec (second part of recipe 7)

  - Repeat steps 10(a-c) one or two more times until development is complete.

- Bake@90C/60sec to further dry out DS2100

- Measure with dektak before curing

- Final Cure in BLUE M Oven:

  - Program#5

  - Purge oven with N2(for 1/2hr)before loading sample for curing

  - Edit the program

  - ramp up to 50C-5min( time in program is 0.05 for 5min)

  - soak@50C-5min

  - ramp up to 100C-15min( time in program is 0.15 for 15min)

  - soak@50C-15min

  - ramp up to 150C-15min

  - soak@150C-15min

  - ramp up to 250C-1hour( time in program is 1.00 for 1hour)

  - soak@250C-1hour

  - Load sample in oven  (using Al boat or on bottom tray directly), DO NOT cover it.

  - Close the door, leave a note that BCB is baking!

  - Make sure N2 in ON( 60-70)

  - Run the program( P5, run)

  - Wait few minutes to check if it is running and if T is going UP!

  - CURING takes 4hours

  - COOLING DOWN takes several  hours (overnight is good)

  - DO NOT OPEN door while it is cooling down!  OK to open at 150C.

- Note:  If you will use metal on the BCB Deposit 1000-1500A SiN on BCB for metal adhesion.